## Slide 1
MATERIALS
AMOURPHOUS
CRYSTALLINE
SUPERSTRUCTURE
QUASICRYSTAL
It can also be in two different form

## Slide 2
Crystal
Crystal
Crystal
Crystal
Crystalline
Quasicrystal
Super structure

## Slide 3
Triclinic
Monoclinic
Orthorhombic
Tetragonal
Cubic
Hexagonal
Rhombohedral
α ≠ β ≠ γ ≠ 900 a ≠ b ≠ c
α (ZY) β(ZX) γ(XY)
α = γ = 900 ≠ β a ≠ b ≠ c
α = β = γ= 900 a ≠ b ≠ c
α = β = γ=900 a = b ≠ c
α = β = γ= 900 a = b = c
α = β = 900 γ=1200 a = b = c
α = β = γ ≠ 900 a = b = c
P
P, C
P, C, F, I
P, I
P, F, I
P
R
1
2
4
2
3
1
1

## Slide 4
Point Group:
a point group is a group of geometric symmetries leaving a point fixed.
32 Point groups
Triclinic
Monoclinic
Orthorhombic
Tetragonal
Cubic
Hexagonal
Rhombohedral
1, 1
2, m, 2/m
222, 2mm, mmm
4, 4, 4/m
422,4mm,4m2,4/m mm
23, m3
432, 43m,m3m
6, 6, 6/m
62, 6mm,6m2, 6/m mm
3, 3
32,3m,3m
1
2/m
mmm
4/m
4/m mm
m3
m3m
6/m
6/m mm
3
3m
In all casees where the incident X-ray wavelength is not near the x-ray absorption edge of the material of the crystal, x-ray diffraction automattically introduces a centre of symmetry. i.e. It can not distinguish between reflection h k l and h k l. It is not possible to find out whether the crystal is centrosymmetrical or not. Hence 32 crystal classes reduce to 11 lau group.
Space group: Lattice type + Point group (230 space groups)

## Slide 5
XRD
The Nobel Prize in Physics 1901 was received by Wilhelm Conrad Röntgen for his great invention of x- ray.
The first X-ray diffraction experiments on a single crystal was carried out in 1912 (Friedrich, Knipping and von Laue)
Now a days X-ray crystallography has been of major importance in natural sciences and especially in crystals.
X-ray diffraction provided the ideal means to understand structures of crystalline matters on an atomic scale.

## Slide 6
Like visible light an X-ray beam is an electromagnetic wave characterized by an electric field vector E which is perpendicular to the direction of propagation and a magnetic field vector H which in turn is perpendicular both to E and the direction of propagation.
The spectra of visible light comprises the range from 4000 to 7000Å , while X-rays have typically wavelengths between 0.1 to 10Å.
Due to the fact that X-ray wavelengths are comparable to the interatomic distances within a crystalline material one observes characteristic interactions between the X-rays and the ordered array of electrons in the crystal structure. These interactions make X-rays the most important source for the investigation of crystal structures.

## Slide 7
X-rays are produced when electrons are accelerated and collide with a target
  Bremsstrahlung x-rays
  Characteristic x-rays
X-rays are sometimes characterized by the generating voltage
  0.1-20 kV soft x-rays
  20-120 kV diagnostic x-rays
  120-300 kV orthovoltage x-rays
  300 kV – 1 MV intermediate energy x-rays
  > 1MV megavoltage x-rays

## Slide 8
Bremsstrahlung x-rays occur when electrons are (de)accelerated in the Coulomb field of a nucleus

## Slide 9
The power radiated from an accelerating charge is given by Larmor’s equation
In the case of an electron in the Coulomb field of a nucleus

## Slide 10
The probability of bremsstrahlung goes as Z2, hence high Z targets are more effective than low Z
The energy of the x-rays varies from zero to the maximum kinetic energy of the electron

## Slide 11
After excitation, ions with a vacancy in their inner shell can de-excite
  Radiatively through x-ray fluorescence
  Non-radiatively through the emission of Auger electrons
Characteristic x-rays

## Slide 12
Thus an x-ray spectrum will also show characteristic x-rays arising from L to K and M to K transitions after ionization of a K electron
  Usually transitions to higher shells absorbed by the filtration or are not x-rays

## Slide 13
Wavelengths in Nanometer Units of Characteristic Emission Lines for Selected Elements.
Element Kα1 Kα2 Kβ1 Lα1
Cr 0.228962 0.229351 0.228480 ****
Cu 0.154051 0.1544330 0.139217 1.3357
Mo 0.070926 0.071354 0.063225 0.54062
W 0.020899 0.021381 0.018436 0.14763

## Slide 14
X-rays by a lattice plane was suggested by W. L. Bragg in 1912 and is known as the Bragg-equation
2dh,k,lsinθ = nλ
λ = wavelengths of the X-rays,
dh,k,l = Interplanar spacing of parallel lattice planes
θ = Diffraction angle

## Slide 15
λ = hc/Ve
V is the voltage drop from filament to target
(K -> L) this radiation is called Kα radiation. If the electron drops from the energy level M to level K the so-called Kβ radiation is emitted.
Filters and Monochromators
Detectors
Single crystal methods
The rotation method, The Weissenberg camera, The Precession camera,
  The automatic single crystal diffractometer

## Slide 16
TECHNIQUES IN THE XRD
• X-ray Powder Diffraction (XRPD)
• Single Crystal Diffraction (SCD)
• Grazing Incidence Angle Diffraction (GIXD)
• X-ray Reflectivity (XRR)
• Small Angle X-ray Scattering (SAXS)

## Slide 17
Bragg-Brentano laboratory diffractometer in reflection geometry with bent (focusing) primary beam monochromator M, primary soller slit P.S.S., divergence slit D.S., scattering slit A.S.S., secondary soller slit S.S.S and receiving slit R.S.

## Slide 18
X-Ray Powder Diffraction (XRPD)
• More appropriately called polycrystalline X-ray diffraction, because it
can also be used for sintered samples, metal foils, coatings and
films, finished parts, etc.
• Used to determine:
– phase composition (commonly called phase ID)- what phases are
present?
– quantitative phase analysis- how much of each phase is present?
– unit cell lattice parameters
– crystal structure
– average crystallite size of nanocrystalline samples
– crystallite microstrain
– texture
– residual stress (really residual strain)
– in-situ diffraction (from 11 K to 1200C in air, vacuum, or inert gas)

## Slide 19
Diffraction angle (2) →
Intensity →
90
180
0
Crystal
90
180
0
Diffraction angle (2) →
Intensity →
Liquid / Amorphous solid
90
180
0
Diffraction angle (2) →
Intensity →
Monoatomic gas
Schematic of difference between the diffraction patterns of various phases

## Slide 21
Instrumental
Crystallite size
Strain
Stacking fault
XRD Line Broadening
Other defects
Unresolved 1 , 2 peaks  Non-monochromaticity of the source (finite width of  peak)
Imperfect focusing
In the vicinity of B
‘Residual Strain’ arising from dislocations, coherent precipitates etc. leading to broadening
In principle every defect contributes to some broadening
Bi
Bc
Bs

## Slide 23
The (pseudo-)Voigt function
Gaussian
Lorentzian
FWMH2 = (U+D2ST)( tan2θ) +V (tanθ) +W+IG/cos2θ
Where U, V and W are the usual peak shape parameters, IG is a measure of the isotropic size effect, DST =coefficient related to strain.

## Slide 24
Scherrer’s formula
 → Wavelength
L → Average crystallite size ( to surface of specimen)
k → 0.94 [k  (0.89, 1.39)], only for circular grain ~ 1 (the accuracy of the method is only 10%)
For Gaussian line profiles and cubic crystals

## Slide 25
Separating crystallite size broadening and strain broadening
Plot of [Br Cos] vs [Sin]
Strain broadening
 → Strain in the material

## Slide 26
Example of a calculation
Sample: Annealed Al Radiation: Cu k ( = 1.54 Å)
Sample: Cold-worked Al Radiation: Cu k ( = 1.54 Å)
2 →
Intensity →
2 →
Intensity →
40
60
40
60
X-Ray Diffraction: A Practical Approach, C. Suryanarayana & M. Grant Norton, Plenum Press, New York (1998)

## Slide 29
(a) Typical Williamson-Hall plot of sample S1 (CoFe2O4: Citrate method) and (b) S2 (CoFe2O4: co-precipitation method) annealed at 600oC. 1% error bar has shown for each data.

## Slide 30
 | S1 (CoFe2O4: citrate method) |  |  | S2 (CoFe2O4: co-precipitation method) |  | 
Annealing temperature | Scherrer’s method | Williamson-Hall method | Rietveld method | Scherrer’s method | Williamson-Hall method | Rietveld method
2000C | 9.1 | 8.1 | 6.2 | 12.1 | 11.2 | 9.4
4000C | 12.2 | 11.1 | 9.3 | 14.3 | 13.1 | 11.1
6000C | 38.3 | 37.1 | 35.4 | 17.4 | 16.3 | 15.3
8000C | 50.1 | 49.2 | 48.2 | 36.1 | 35.1 | 33.2
Average crystallite size (nm) calculated by Scherrer’s, Williamson-Hall and Rietveld methods for the samples S1 and S2 annealed at different annealing temperatures.

## Slide 31
X-ray Scattering by assemblies of electrons
Fourier transform
Convolution Product
X-ray scattering by particles in solution.

## Slide 33
This is a generic function where G, Rg, P and B are defined according to local functions. For example, for a sphere, G = N n2; Rg = R/1.3; P = 4; B = 2p G S/V2 = 9 G/(2 R4). (Sphere S = 4πR2; V = 4πR3/3)

## Slide 34
What is Grazing Incidence Diffraction?
Grazing Incidence Diffraction for Thin Film Phase Analysis
X-ray radiation has a large penetration depth into any matter. Due to this property X-ray diffraction is not surface sensitive
Grazing Incidence Diffraction (GID) is the technique to overcome this restriction.
GID measurements are performed at very low incident angles to maximize the signal from the thin layers. This allows Phase analysis on very thin layers
Surface sensitivity down to nm scale
Depth profiling of the phase composition of layered samples Göbel Mirrors for incident and diffracted beam with enhanced sensitivity and shorter measurement times Crystallography of thin films

## Slide 35
Why use GID?
It is sometimes very difficult to analyze thin films due to their small diffracting volumes, which result in low diffracted intensities compared to the substrate and background.
This combination of low diffracted signal and high background make it very difficult to identify the phases present.
Accordingly, special techniques must be used when analyzing thin films
The most common technique for analyzing films as thin as 10nm is to use a grazing incidence angle arrangement combined with a parallel beam geometry
By increasing the path length of the incident X-ray beam through the film, the intensity from the film can be increased so that conventional phase identification analysis can be run.

## Slide 37: XRR Curve of a Periodic Multilayer
Total reflection  Electron density of the uppermost layer
Decrease of the reflected Intensity  interface roughness
Kiessig oscillations  thickness of the whole multilayer
Bragg-like peaks  thickness of the periodic motif
Extinction of the Bragg-like peaks  thickness of the individual layers in the multilayer system

## Slide 38: Fe/Au Multilayers Experimental example
t (Fe) (27 ± 2) Å
t (Au) (23 ± 1) Å
L 50 Å
s (Fe) 5 Å
s (Au) 5 Å
r (Fe) (1.4 ± 0.2)
(Au) (0.9 ± 0.1)
Fe/Au (27Å/23Å)x10
Si/Au(100Å)
Refined parameters

## Slide 39: X-ray reflectivity measurement
Si
Mo
Mo
Mo
r t [Å] s [Å]
0.68 19.6 5.8
0.93 236.5 34.0
1.09 14.1 2.7
1.00 5.0 2.7
1.00 2.8
Calculation of the electron density, thickness and interface roughness for each particular layer
W
The surface must be smooth (mirror-like)
Edge of TER
Kiessig oscillations (fringes)

## Slide 40
Thin Film analysis by X-Ray Scattering: Mario Birkholz
Cullity, B. D
Elements Of X Ray Diffraction
X-Ray Diffraction
BE Warren

## Slide 41
SPECTROSCOPIC METHODS
UV-VIS Spectrophotometer: Absorption and Emission
Interaction of Electromagnetic Radiation (EM) with Mater: Spectrum
The interaction of radiation with matter assumes many forms. Molecular absorption of radiation is described by
Nanomaterial Interact with UV-> Many effects->
Plasmon oscillations on the surface of nanomaterials
Electron transfer cascades
Exciton Pairs in semiconductors (nano-TiO2)
Particle size dependent fluorescence (semiconductor quantum dots)
Diameter dependent fluorescence (SWCNT)
Interference colors (porous alumina or titania thin films)
Beer-Lambart law

## Slide 42
On the left, most of the visible light is reflected from a bulk metal surface. For example, the absorption–reflection of light is why bulk gold appears to have a yellow-reddish cluster. The middle image depicts how a thin particulate metal film (beyond the percolation threshold) scatters and reflects light. Some light is transmitted, some absorbed, and some reflected. The color of a thin film of Au may appear green if it is microgranular. On the right, a large fraction of the light is transmitted and scattered through a transparent
nanometal composite material. Absorption of light by nano gold yields many colors, depending on the size, shape, and orientation of the particle and the dielectric function of the surrounding medium.

## Slide 43
UV-visible spectrum of a typical Au NPs solution in the presence of AA in aqueous medium.
The UV-visible spectrum of AgNO3 added Au NP solutions
Dependence of the absorption maxima (λmax) of the Ag and Au NPs

## Slide 44
Infrared and Raman Spectroscopy
Rely on Vibrational Energy: IR rely on asymmetrical (dipolar) vibration and Raman rely on Symmetrical (polarizable) vibrations. Complement each other
Raman spectroscopy is extremely inefficient: only 1 in 108 photons are Raman scattered and typical scattering cross sections are ~10-30 cm2 (12 orders of magnitude less than
IR, 10-18 cm2 and 15 less than fluorescence excitation,10-15cm2 ).
Raman Spectroscopy Involves excitation with monochromatic laser light. Inelastically scattered light is the carrier wave for molecular vibrations— lower energy (Stokes lines) and higher energy (anti-Stokes lines). Usually Stokes lines are seen.
Conventional Raman spectroscopy
Resonant Raman spectroscopy
Surface Enhanced Raman spectroscopy
Surface Enhanced Resonant Raman spectroscopy

## Slide 46
Surface Enhanced Raman SpectroscopySERS
Surface enhanced Raman spectroscopy is a true nanobased method.
The effect is related directly to nanoparticles or nanofacets (roughened) on a surface.
The plasmon electron cloud is responsible for most of the enhancement.
The plasmon exists on the surface of metals— nano (localized) and bulk (delocalized).
In nanometals, the surface plasmon is localized and the “degree” of interaction depends on the size, orientation and type of metal of the nanoparticle
• Electromagnetic theory of SERS is simple and can account for all SERS observations. It is wavelength specific
• Nanomaterials are required for SERS-active systems
• Some metals (noble metals) are good SERS substrates,others not
• The incredible signal enhancement (up to 1015) is due mostly to the electromagnetic properties of certain noble metal nanoparticles and allows for detection of single molecules
• Quantum theory not absolutely necessary to explain SERS effect

## Slide 47
There are two modes of signal enhancement:
Electromagnetic Enhancement is linked to excitation of the surface plasmon. Plasmons are electromagnetic waves that propagate along the metal-dielectric interface as a result of the motion of electrons upon stimulation. When the analyte
molecule is placed within the proximity of the plasmon, it experiences an enhanced electric field and produces an enhanced scattering Raman field— leading to and enhanced analytical signal.
Chemical Enhancement involves charge transfer between the analyte chemisorbed species and the metal. New charge transfer pathways (new energy levels) are created that open the door for resonant SERS.

## Slide 49
Raman intensity conforms to a ν4 dependence. In other words, the higher the frequency (shorter the wavelength), the better the intensity of the analytical signal.
In SERS, there is no ν4 dependence. Actually, lower frequency molecular vibrations are enhanced better than higher frequency vibrations due to the frequency dependence of the plasmon resonance.
Overall, SERS signals are relatively independent of the laser’s frequency and acquisition can occur at several different laser “colors”.
Bulk Surfaces:
Roughened surface (nano-facets) → 103 to 106 enhancement
Nanoparticles:
Enhancement tuned to size of nanoparticle
Enhancement tuned to shape of nanoparticle
Enhancement tuned to orientation of nanoparticle

## Slide 50
Case 1:
When the electric field of the light is aligned parallel to the long axis of the nanoparticle, its “hot spot” is maximized (e.g. the “lightning rod” effect). This leads to a maximized SERS effect. An analyte molecule that is chemisorbed onto this site will deliver a large SERS signal. A clear polymer embedded with nanoparticulate gold in this orientation will appear to be green.
Case 2:
When the short axis of the nanoparticle is aligned with the electric field, the SERS enhancement is minimized. A clear polymer embedded with such nanoparticulate gold with this orientation will appear to be red.

## Slide 51
THERMODYNAMIC METHODS
Brunauer-Emmett-Teller (BET)
• Thermal gravimetric analysis (TGA) → Δm
• Differential thermal analysis (DTA) → ΔT
• Differential scanning calorimetry (DSC) → ΔH
• Thermomechanical analysis (TMA) → Δ dimension
• Dynamic mechanical analysis (DMA) → damping
• Dilatometry → ΔV

## Slide 52
One tried and true analytical method grounded in traditional thermodynamics (and nanoscience) is the BET method to determine surface area and porosity. Gas sorption methods are applied to determine surface area, specific surface area, pore volume, pore size distribution and active sites. Adsorption is the accumulation of an adsorbate on a surface (the
adsorbent).
Physisorption is a non-specific process dominated by van der Waals forces, therefore, the heats of adsorption of generally small: ΔHads = 10 – 40 kJ·mol-1 and the process occurs at low temperatures (77 K for N2). Chemisorption involves the forming of chemical bonds (ΔHchem = 100 – 400 kJ·mol-1).
The level of adsorption depends on the temperature, the pressure, the interaction between the gas and the solid and the total amount of surface area.
There are many kinds of adsorption isotherms. We will only consider the BET isotherm that is applicable to Type II isotherm (no pores) but fits Types I and IV isotherms as well.

## Slide 53
The Fundamental Equation of BET:
where P is the equilibrium pressure of the adsorbate (usually N2) and Po is the reference saturation pressure at the ambient temperature; ᶹ is the amount of adsorbed gas and ᶹm is the amount of physisorbed gas in the monolayer, both in terms of L
c is a constant relates the energies of adsorption (Eabs) and condensation (Econd)
Assumptions of BET
1. The surface energy is homogeneous
2. Only the top layers of the adsorbate are in equilibrium with the vapor (vertical interactions)
3. Lateral interactions of adsorbate condensate are not considered

## Slide 55
BET isotherm (with porosity and Hysteresis) with its extracted BET line. The specific surface area was
determined by the amount of adsorbate per monolayer.
BJH (Barnett-Joyner- Halenda) and DFT (density functional theory) analysis yields information about
pore volume and pore size. An Autosorb-I Series surface area analyzer manufactured by Quantachrome Instruments is depicted.