## Slide 1: Nanocomposites
Composite materials are made from two or more materials with significantly different physical or chemical properties, that when combined, produce a material with characteristics different from the individual components.
The individual components remain separate and distinct within the finished structure.
There are four types:
  1. Fibrous composites (fibers in a matrix)
    Continuous fibers, woven fibers, chopped fibers
  2. Laminated composites (layers of various materials)
  3. Particulate composites
  4. Combinations of some or all of the above

## Slide 2
Color online Schematic illustration of three composites with the three common connectivity schemes: (a) 0–3 particulate composite, (b) 2–2 laminate composite, and (c) 1–3 fiber/rod composite.

## Slide 3
Surface area/volume (A/V) relations for various reinforcing geometry
d is the particle or fibre diameter,
l -> fibre or platelet length
t ->platelet thickness
homogeneous nanocomposite should be created more easily using nanofibres rather than nanoplatelet
Nanocomposites consist of a nanometer-scale phase in combination with another phase. In terms of nanofiller dimensionality, they can be classified as zero dimensional nanosphere), one-dimensional (nanofibre), two-dimensional (nanoplatelet), and three-dimensional (interpenetrating network) systems

## Slide 4: Advantages of Nanosized Additions
Mechanical properties e.g. strength, modulus and dimensional stability
Decreased permeability to gases, water and hydrocarbons
Thermal stability and heat distortion temperature
Chemical resistance.
Surface appearance
Electrical conductivity
Magnetic property
Optical clarity in comparison to conventionally filled polymers

## Slide 5: Disadvantages of Nanosized Additions
Impurity
Cracks.
Toughness and impact performance

## Slide 6
Multiferroics
If a magnetic field is applied to these material
for the piezoelectric phase; where S is the strain and em and e are, respectively, piezomagnetic and piezoelectric coefficients. As a result, this two-phase composite material can be
characterized by
where kc is a coupling factor 0≤kc≤1 between the two
phases and is the ME coefficient of the composite.
a new property i.e., nonzero ME coefficient appears in the composite consisting of magnetic and piezoelectric phases, since neither constituent phase is magnetoelectric. This new ME product response is due to elastic coupling between the two constituent phases. High piezomagnetic and
piezoelectric coefficients and strong coupling large kc favor a large ME coefficient.
Let us take one EXAMPLE
Similarly enhancement of dielectric property, magnetic property, electrical transport etc.

## Slide 7
Stiffness E1 (Rule of Mixtures)
MATRIX
MATRIX
fiber

## Slide 8
COMPOSITE
Stiffness E2 (Rule of Mixtures)
MATRIX
MATRIX
fiber
Stiffness n12 and G12

## Slide 9
For composites in which discontinuous fibres are not perfectly aligned, two parameters need to be incorporated in equation, the length efficiency factor(ηL ) and the orientation factor(η0)
The fibre length efficiency factor ηL can vary between 0 and 1
The orientation factor η0 is equal to 1 for fully aligned fibres
3/8 for random two dimensional orientation
1/5 for three dimensional orientation
A similar equation is valid for strength,

## Slide 10
Strength prediction: In general, relations for predicting strength are complex. However, for randomly oriented fibers, an approximate equation may be used to estimate the tensile strength, as follows (Gibson, 2007):

## Slide 11
LET US NOTE DOWN DIFFERENCES BETWEEN COMPOSITE AND NANOCOMPOSITE
Nanocomposite:
~ 10% filler compare to the matrix (polymer, ceramic, metal etc.)
Strength of Matrix definitely increase, similar to other properties.
Composite:
Any combination
Strength of Matrix may or may not increase. Similar to other properties.

## Slide 12
Engineering Applications:
1. Composite materials or nanocomposite have been used in aerospace, automobile, and marine applications
2. Composite materials in civil engineering structures
3. seismic retrofit of bridge columns, replacements of deteriorated bridge decks, and new bridge structures.

## Slide 13
Medical Applications:
Stents are made with steel or with polymers with shape memory effects
(The material is deformed within a temperature range of glass transition temperature (Tg) of amorphous phase and melting temperature (Tm) of crystalline phase, then was cooled below Tg. After the material was reheated between Tg and Tm, the original structural shape was recovered)

## Slide 14
Flexibility.
Easy processing.
Low weight.
Relatively high electrical breakdown strength(≈ 100MV/cm) as compare to ceramic (10-100kV/cm).
C
n
CH2
H
OH
Polyvinylidene Fluoride
[PVDF]
Polyvinyl Alcohol
[PVA]
Poly(methyl methacrylate)
[PMMA]
Melting Point: 160oC
Density : 1.18 g/cm3
Melting Point: 200oC
Density : 1.19 g/cm3
Melting Point: 178oC
Density : 1.78 g/cm3
Chemical structure of the different polymers a) PVDF b) PVA and c) PMMA
Why Polymer?

## Slide 15
Introduction to Polymer Nanocomposite
Combination of a polymer matrix and inclusions (filler) that have at least one dimension (i.e. length, width or thickness) in the nanometre size range.
Nanoparticles (3D)
Nanosheets (2D)
Nanowire (1D)
Polymer Network
Progress in Materials Science 57 (2012) 724–803

## Slide 16
Several issues need to be address
  Physical dispersion
  Optimization of nanofiller to matrix ratio under percolation threshold limit.
  Shape and size of nanofillers
  Fabrication processes.
  Type matrix (polymer) and filler (nanoparticle)
Advantages
  Low filler loading.
  Large surface area.
  Without sacrificing the density, flexibility .
  Enhance the physical and chemical properties.
Scientific Reports 6, (2016), 26198, Journal of Alloys and Compounds 551 (2013) 200-207
Advantage of Ceramic-Polymer nanocomposite
Polymer nanocomposite

## Slide 17
Nanofiller
Matrix
Interphase
Schematic diagram of nanocomposite
Enhance the interface area in nanocomposite due to nanosize filler, which leads to
Improve polarization and polarizability at the interface
PLASMONIC EFFECT OF NANOMATERIAL
Alter the electrochemical and electromechanical properties .
Role of nanomaterial- polymer interface in nanocomposites

## Slide 19
a
b
d
c
e
f
Expected structure and BLCs model of (1-x) PVDF(x)-BHF for x= (a) 0.00, (b) 0.025, (c) 0.05, (d) 0.15, (e) 0.30 and (f) 0.50.

## Slide 20
Polymer nano-
Composites
Energy harvesting & storage
EM Radiation
absorption
Sensing & Actuation
Transportation & safety
Defense sector
Information Industry
Novel Catalysts
Environmental remediation
Different applications of Polymer nanocomposite
Applications of Polymer nanocomposites

## Slide 21
Flexibility.
Easy processing.
Low weight.
Relatively high electrical breakdown strength(≈ 100MV/cm) as compare to ceramic (10-100kV/cm).
C
n
CH2
H
OH
Polyvinylidene Fluoride
[PVDF]
Polyvinyl Alcohol
[PVA]
Poly(methyl methacrylate)
[PMMA]
Melting Point: 160oC
Density : 1.18 g/cm3
Melting Point: 200oC
Density : 1.19 g/cm3
Melting Point: 178oC
Density : 1.78 g/cm3
Chemical structure of the different polymers a) PVDF b) PVA and c) PMMA
Why Polymer?

## Slide 22
Polymer Nanocomposite
Combination of a polymer matrix and inclusions (filler) that have at least one dimension (i.e. length, width or thickness) in the nanometre size range.
Nanoparticles (3D)
Nanosheets (2D)
Nanowire (1D)
Polymer Network
Progress in Materials Science 57 (2012) 724–803

## Slide 23
Several issues need to be address
  Physical dispersion
  Optimization of nanofiller to matrix ratio under percolation threshold limit.
  Shape and size of nanofillers
  Fabrication processes.
  Type matrix (polymer) and filler (nanoparticle)
Advantages
  Low filler loading.
  Large surface area.
  Without sacrificing the density, flexibility .
  Enhance the physical and chemical properties.
Scientific Reports 6, (2016), 26198, Journal of Alloys and Compounds 551 (2013) 200-207
Advantage of Ceramic-Polymer nanocomposite
Polymer nanocomposite

## Slide 24
Nanofiller
Matrix
Interphase
Schematic diagram of nanocomposite
Enhance the interface area in nanocomposite due to nanosize filler, which leads to
Improve polarization and polarizability at the interface
PLASMONIC EFFECT OF NANOMATERIAL
Alter the electrochemical and electromechanical properties .
Role of nanomaterial- polymer interface in nanocomposites

## Slide 25
Polymer nano-
Composites
Energy harvesting & storage
EM Radiation
absorption
Sensing & Actuation
Transportation & safety
Defense sector
Information Industry
Novel Catalysts
Environmental remediation
Different applications of Polymer nanocomposite
Applications of Polymer nanocomposites